## Slide 1
Development of Integrated Solar-Fuel Generators
Carl Koval
Basic Energy Sciences Advisory Committee Meeting
February 27, 2014

## Slide 2: Overview
Fuels from Sunlight: A Grand Challenge
The Sun is a singular solution to our future energy needs - capacity dwarfs fossil, nuclear, wind . . . - sunlight delivers more energy in one hour than the earth uses in one year - free of greenhouse gases and pollutants - secure from geo-political constraints
Enormous gap between our tiny use of solar energy and its immense potential
- Incremental advances in today’s technology will not bridge the gap - Conceptual breakthroughs are needed that come only from high risk-high payoff basic research
Interdisciplinary research is required - Physics, chemistry, biology, materials, nanoscience
Basic and applied science should couple seamlessly
Take the “Beat-the-Leaf” Challenge

## Slide 3: Overview
JCAP Mission
JCAP’s Mission is to demonstrate a scalably manufacturable solar-fuels generator using Earth-abundant elements that, with no wires, robustly produces fuel from the Sun ten times more efficiently than (current) crops.
Natural Photosynthesis
Artificial Photosynthesis
“It is time to build an actual artificial photosynthetic system, to learn what works and what does not work, and thereby set the stage for making it work better”
Melvin Calvin (1961 Nobel Laureate)

## Slide 4: Overview
General Approaches to Artificial Photosynthesis
Key requirements from technoeconomic analysis: efficiency, module cost, stability, safety
1 G. Peharz, F. Dirmouth, and U. Wittstadt Int. J. of Hydrogen Energy 2007, 32, 3248-3252 (DOI: 10.1016/j.ijhydene.2007.04.036)
Discrete Photovoltaic Wired to Electrolyzer
Advantages: Operational system has already been demonstrated with 18% electrochemical efficiency.1
Challenges: Demonstrated system demands expensive components; lack of integration further reduces cost efficiency.
Integrated Photoelectrochemical Solar-Fuel Generator
Solar-Fuel Generating Particle Dispersions
Advantages: Offers a simple architecture with the potential for low materials cost.
Challenges: Low efficiency and co-generation of fuel and oxidizer pose operational safety issues.
Advantages: Potentially lower component costs than a discrete system with reduced complexity.
Challenges: Requires that semiconductor, catalysts, and membranes operate efficiently under identical conditions.
H2
O2
H2O
Semiconductor nanoparticle
Catalyst

## Slide 5: Overview
An Integrated Approach to Artificial Photosynthesis
JCAP System Concept
Fuel Forming Reactions
Hydrogen production
H2O H2 + ½O2
Hydrocarbon production
CO2 + H2O HCOOH + ½O2
CO2 + H2O HCHO + O2
CO2 + 2H2O CH3OH + 3/2 O2
CO2 + 2H2O CH4 + 2O2

## Slide 6: Overview
JCAP’s Original Concept for an Integrated Solar-Fuel Generator
Key requirements from technoeconomic analysis: efficiency, module cost, stability, safety
Tandem light absorbers
Fuel and oxygen catalysts
Ion-conducting,
gas-separation membrane
Radial collection of photogenerated carriers

## Slide 7: Overview
Acid-Stable Embedded Microwire Array
Core-Shell Tandem Junction Microwire Arrays
50 μm
100 μm
Alkaline-Stable Embedded Microwire Array

## Slide 8: Overview
Systematic Approach to Solar-Fuel Generator Prototypes
Integrated prototype
devices
Assemblies and processes
Materials discovery
• High-throughput materials discovery
• Programs at DOE user facilities
• Design, fabrication and testing of prototypes
• Simulation and modeling of solar-fuels generators
Critical Enabling capabilities and partnerships
• Interdisciplinary problem-solving teams
• Performance benchmarking of light absorbers and catalysts

## Slide 9: Integrated Prototype Devices
Systematic Approach to Solar-Fuel Generator Prototypes
Integrated prototype
devices
Assemblies and processes
Materials discovery
Detailed modeling of prototype design space
Fabrication, assembly, and testing
Comprehensive design of prototypes
Conceptual design of pre-prototypes

## Slide 10: Integrated Prototype Devices
Early Prototyping Efforts in the Aviation Industry

## Slide 11: Integrated Prototype Devices
Example Pre-Prototype Concepts
Conceptual design of pre-prototypes
Electrolyte re-circulator
Vapor feed device
Photovoltaic / membrane-electrode-assembly
Louvered device
Membrane-free device
Side-by-side photovoltaic/electrolyzer

## Slide 12: Integrated Prototype Devices
Prototype That Enables Continuous H2 Production Under Near-Neutral Conditions
Recirculation of the supporting electrolyte in a water-splitting solar-fuel device eliminates large overpotentials and pH gradients
Miguel A. Modestino, Karl A. Walczak, Alan Berger, Christopher M. Evans, Sophia Haussener, Carl Koval, John S. Newman, Joel W. Ager, and Rachel A. Segalman Energy Environ. Sci. 2014 (DOI: 10.1039/C3EE43214A)
Dependence of Overpotential and pH on Recirculation Rates
Recirculating Solar-Fuel Generator
Without recirculation, the potential needed to maintain a fixed current density increases dramatically.
Large pH gradients associated with the depletion of buffer ions are minimized with recirculation
Recirculation can be used to mitigate the build up of supporting electrolyte ions, which under moderate pH conditions, is necessary for ion transport
Conceptual design of pre-prototypes

## Slide 13: Integrated Prototype Devices
JCAP Modeling Overview
from ab initio electronic structure calculations for materials to multidimensional modeling of solar-fuels prototypes
Theory
Modeling
0-D
1-D
Multidimensional
Light absorption
Electronic transport
Electronic structure/energy calculations for photoabsorbers and surface-attached linkers
Solution transport
Catalysis
Electronic structure/energy calculations for heterogeneous and molecular catalysts
H+
H2
O2

## Slide 14: Integrated Prototype Devices
Modeling Thermal Effects on Solar-Fuel Generators
Sophia Haussener, Shu Hu, Chengxiang Xiang, Adam Z. Weber, and Nathan S. Lewis “Simulations of the Irradiation and Temperature Dependence of the Efficiency of Tandem Photoelectrochemical Water-Splitting Systems” Energy Environ. Sci. 2013, 6, 3605-3618. (DOI: 10.1039/c3ee41302k)
Detailed modeling of prototype design space
Efficiency Modeling of Prototype Designs
Comparison of instantaneous efficiency for four typical seasonal days under three isothermal conditions
Comparison of normalized annually integrated fuel production

## Slide 15: Integrated Prototype Devices
Modeling the Efficiencies of Solar-Fuel Generators
Shu Hu, Chengxiang Xiang, Sophia Haussener, Alan D. Berger, and Nathan S. Lewis “An Analysis of the Optimal Band Gaps of Light Absorbers in Integrated Tandem Photoelectrochemical Water-Splitting Systems” Energy Environ. Sci. 2013, 6, 2984-2993. (DOI: 10.1039.c3ee40453f)
Detailed modeling of prototype design space
Modeling of Solar-to-Hydrogen Efficiencies
Isoefficiency plot for prototype configuration A: photoanode + photocathode photoelectrochemical cell
Isoefficiency plot for prototype configuration B: tandem absorber + electrocatalyst

## Slide 16: Assemblies and Processes
Systematic Approach to Solar-Fuel Generator Prototypes
Integrated prototype
devices
Materials discovery
Assemblies and processes
Light-absorber / catalyst interfaces
Light-absorber / membrane interfaces
Light-absorber junctions
3D mesoscale architectures

## Slide 17: Assemblies and Processes
Discovery and Integrated System Development In JCAP
Underpinning Discovery Science
Component Assembly and Optimization
Scale-up and System Integration
Accelerated Materials Discovery
Process and Materials Integration Team (PMIT)

## Slide 18: Assemblies and Processes
Acid-Stable Embedded Microwire Array
Core-Shell Tandem Junction Microwire Arrays
50 μm
100 μm
Alkaline-Stable Embedded Microwire Array

## Slide 19: Assemblies and Processes
3. Deposit SC/SC contact
Si wire
FTO
2. Metallurgical junction formation in Si
SiO2 “Boot”
10 μm
Fabrication of Core-Shell Tandem Junction Microwire Arrays
Matthew M. Shaner, Katherine T. Fountaine, Shane Ardo, Rob H. Cordian, Harry A. Atwater, Nathan S. Lewis Energy Environ. Sci. 2014, 7, 779-790. (10.1039/c3ee43048k)
1. Si microwire growth via Cu catalyzed VLS-CVD method
n+-Si
50 μm

## Slide 20: Assemblies and Processes
5. Membrane embedment, substrate removal, and catalyst deposition
100 μm
5 μm
Fabrication of Core-Shell Tandem Junction Microwire Arrays
Matthew M. Shaner, Katherine T. Fountaine, Shane Ardo, Rob H. Cordian, Harry A. Atwater, Nathan S. Lewis Energy Environ. Sci. 2014, 7, 779-790. (10.1039/c3ee43048k)
4. Deposition of WO3 or TiO2
30 μm
Si
FTO
TiO2
2 μm

## Slide 21: Assemblies and Processes
Discovery of Inherently Stable Light Absorbers
Approaches to Achieving Stable Light Absorber/Catalyst Assemblies
Surface Protection of Unstable Light Absorbers
Acid- or base- stable
Discover 1.7-2.2 eV materials: theory, HTE and directed efforts
Crystalline TiO2, SrTiO3, WO3 and Fe2O3
Raising O 2p level vs. stability?
Chen and Wang, Chemistry of Materials 2012 24 (18), 3659-3666
Hu and Lewis, Science 2014, submitted.
e.g. Si, III-Vs (GaAs, GaP, InP, ternary), CIGS, BVO, CdSe, etc.
Universal protective coatings / protection strategy
“Linker” or “Interfacial layer” for catalyst integration

## Slide 22: Assemblies and Processes
Stabilization of an Efficient, Earth-Abundant Light Absorber
TiO2 coatings protect amorphous Si photocathodes from corrosion, allowing for efficient hydrogen production
Yongjing Lin, Corsin Battaglia, Mathieu Boccard, Mark Hettick, Zhibin Yu, Christophe Ballif, Joel W. Ager, and Ali Javey Nano Lett. 2013, 13, 5615-5618. (DOI: 10.1021/nl403265k)
Structure of TiO2-protected Amorphous Si
Configuration of TiO2-protected photocathode
False-color scanning electron microscope image of TiO2 protection layer (green) deposited on top of amorphous Si layer (red) grown on top of ZnO substrate (yellow).
Performance and Stability of TiO2-protected Amorphous Si Photocathode Assembly
One sun illumination yields significant photocurrent (11.6 mA/cm2)
Over 12 hours, photocurrents of protected samples decay less than 5% (vs. ~90% for unprotected electrodes)

## Slide 23: Assemblies and Processes
40 Years of Attempts to Protect Semiconductor Surfaces
Transparent Conductive Oxides
TiO2 Tunnel Barriers
Redox active barrier layers (e.g. NiOx )
Miller et al. Int. J. Hydrogen Energy (2004); Reece et al. Science (2011).. Kenny Dai et al. Science (2014) Scheuermann et al., Energy Environ. Sci., 2013.
1M KOH
pH=14

## Slide 24: Assemblies and Processes
Photoanode / Catalyst Assembly for Water Oxidation
Atomic-layer deposition of cobalt oxide on n-BiVO4 (Eg = 2.2 eV) produces an alkaline-stable photoanode
Michael F. Lichterman, Matthew R. Shaner, Sheila G. Handler, Bruce S. Brunschwig, Harry B. Gray, Nathan S. Lewis, and Joshua M. Spurgeon J. Phys. Chem. Lett. 2013, 4, 4188-4191. (DOI: 10.1021/jz4022415)
Light-absorber / catalyst interfaces
Cobalt oxide layers were deposited by atomic layer deposition onto n-BiVO4 electrodes
Measurements made at pH=13
CoOx overlayers improve the stability of observed photocurrent

## Slide 25: Assemblies and Processes
development of a stabilizing catalyst film on silicon photoanodes
Jinhui Yang, Karl Walczak, Eitan Anzenberg, Yuan Ping, Jeffrey Beeman, Schwartzberg, Yongjing Lin, Mark Hettick, Ali Javey, Joel Ager, Junko Yano, Heinz Frei, and Ian Sharp 2014, submitted.
Es
Performance under Alkaline Conditions
Photoanode Preparation Process
Stability under Alkaline Conditions
At 10 mA/cm2, the overpotential remains stable for at least 24 hours at pH=13.6.
Catalyst
n-Si
p+-Si
(1) Nanotexturing by Ar sputtering
(2) CoOx deposition by atomic layer deposition
n-Si
n-Si
p+-Si
p+-Si
Photocurrents reach 17 mA/cm2 at 1.23 vs. RHE

## Slide 26: Assemblies and Processes
Development of an integrated protective coating and catalyst for water oxidation
Shu Hu, Matthew Shaner, Joseph Beardslee, Michael Lichterman, Bruce S. Brunschwig, and Nathan S. Lewis “Quantitative, Sustained, Efficient Solar-Driven Oxidation of H2O to O2(g) Using Thin Ni Electrocatalytic Films on TiO2-Coated Si, GaAs, and GaP Semiconductor Photoanodes” 2014, submitted.
Performance
Efficiency is equivalent to a 9.5% efficient photovoltaic in series with an electrolyzer
Photocurrent is stable for more than 100 hours
Stability
OH-
~100 nm TiO2
e-
h+
h+
h+
e-
e-
OH-
OH-
O2
O2
O2

## Slide 27: Assemblies and Processes
Development of an integrated protective coating and catalyst for water oxidation
Continued
Shu Hu, Matthew Shaner, Joseph Beardslee, Michael Lichterman, Bruce S. Brunschwig, and Nathan S. Lewis “Quantitative, Sustained, Efficient Solar-Driven Oxidation of H2O to O2(g) Using Thin Ni Electrocatalytic Films on TiO2-Coated Si, GaAs, and GaP Semiconductor Photoanodes” 2014, submitted.
.
Quantitative Oxygen Evolution
Si
TiO2
Ni
Depth Profiling
Intermixing occurs at the TiO2 / Ni interface

## Slide 28: Materials Discovery
Systematic Approach to Solar-Fuel Generator Prototypes
Integrated prototype
devices
Light absorbers
Basic discovery science
Assemblies and processes
Materials discovery
Benchmarking
High throughput discovery
Catalysts

## Slide 29: Materials Discovery
Overview of Benchmarking Project
Design of benchmarking standards and protocols
Benchmarking of electrocatalysts
Benchmarking of light absorbers
Project Leaders
Approach
Jonas Peters
Tom Jaramillo
Objectives
The Benchmarking Project serves as a community resource for the performance validation of electrocatalysts and photocatalysts. By employing a standard set of measurement protocols, unbiased evaluation by the Benchmarking Project provides comparisons that are as accurate as possible between materials/devices coming from different laboratories.

## Slide 30: Materials Discovery
Development of Methodology for Catalyst Benchmarking
Benchmarking protocols and standards have been established for electrodeposited catalysts
Charles C. L. McCrory, Suho Jung, Jonas C. Peters, and Thomas F. Jaramillo “Benchmarking Heterogeneous Catalysts for the Oxygen Evolution Reaction” J. Am. Chem. Soc. 2013, 135, 16977-16987. (DOI: 10.1021/ja407115p)
Catalyst Benchmarking Protocol
Catalytic activity and stability can now be assessed by measuring electrochemical behavior under standardized conditions
Activity and Stability Measurements

## Slide 31: Materials Discovery
Validation of Catalytic Activity for OER and HER Catalysts
Over 40 electrodeposited catalysts have been benchmarked to date
Catalyst Activity / Stability

## Slide 32: Materials Discovery
Overview of the High-Throughput Experimentation Project
JCAP’s High-Throughput Experimentation (HTE) Project focuses on automated, high-throughput discovery of light absorbers and heterogeneous catalysts. The project employs combinatorial techniques that can produce new alloys from Earth abundant elements, rapid screening methods that can identify high-performing light absorbers and catalysts, and surface-science analysis tools that can characterize the structure and composition of promising materials.
Combinatorial materials synthesis
Project Leader
Approach
John Gregoire
Objectives
High-throughput screening
High-throughput characterization
Planning and analysis

## Slide 33: Materials Discovery
Combinatorial Materials Synthesis
Discrete composition libraries are produced using ink jet printers
Mapping of Composition Space
Ink Formulation and Printing
Calcination
4-element space
3.33% intervals.
5456 samples (1mm2) on 3 plates
Material libraries consisting of pseudo- binary, tertiary, and quaternary compositions can be produced with unprecedented throughput using inkjet printers

## Slide 34: Materials Discovery
Combinatorial Materials Synthesis
Continuous composition libraries can be produced using physical vapor deposition
Off-Axis Sputtering System
Ternary Library Examples
Material libraries consisting of pseudo- binary, tertiary, and quaternary compositions can be produced with physical vapor deposition methods
Metal nitride library
Metal oxide library
Zn
Si
Sn
V
Fe
Bi

## Slide 35: Materials Discovery
Example Screening Tool: Bubble Screening System for Catalyst Activity
Rapid parallel screening of bubbles provides
Chengxiang Xiang, Santosh K. Suram, Joel A. Haber, Dan W. Guevarra, Ed Soedarmadji, Jian Jin, and John M. Gregoire ACS Combi. Sci. 2014,16, 47-52. (DOI: 10.1021/co400151h)
Bubble Screening of Catalyst Libraries
Catalytic activity

## Slide 36: Materials Discovery
Example Screening Tool: High-Throughput Electrochemical Screening
Scanning droplet cell offers unprecedented speed for electrochemical measurements
J. M. Gregoire, C. Xiang, X. Liu, M. Marcin, and J. Jin Rev. Sci. Inst. 2013, 84, 024102. (DOI: 10.1063/1.4790419)
Scanning Droplet Cell
Current-voltage curve
Full 3-electrode electrochemical and photoelectrochemical measurements can be performed to screen potentially promising catalysts and light absorbers.
Collection of current/voltage curve and translation to next library position can be performed in under 4 seconds.

## Slide 37: Materials Discovery
Example Screening Tool: High-Throughput Electrochemical Screening (continued)
Scanning droplet cell serves as a rapid screening tool for oxygen evolution catalysts
J. M. Gregoire, C. Xiang, X. Liu, M. Marcin, and J. Jin Rev. Sci. Inst. 2013, 84, 024102. (DOI: 10.1063/1.4790419)
Mapping of Catalytic Activity for Oxygen Evolution
Entire libraries of catalysts can be screened to identify the highest performing catalysts as a function of composition.
Composition library produced by inkjet printing
Current density measured at 450 mV overpotential as a function of position on composition library
Current density measured at 450 mV ovepotential as a function of position in composition space

## Slide 38: Materials Discovery
Images of Ink-Jet Printed Materials
Transition of High-throughput Materials to Benchmarking
Promising catalyst materials are being benchmarked
Standard HTE composition library on FTO glass (4” x 6”)
Standard benchmarking electrode on glassy carbon (5 mm diameter)
Catalysts that are discovered through the High-Throughput Experimentation Project are further developed for benchmarking.

## Slide 39: Materials Discovery
Discovery of a High-Performing Cerium-Rich Oxygen Evolution Catalyst
Joel A. Haber, Yun Cai, Suho Jung, Chengxiang Xiang, Slobodan Mitrovic, Jian Jin, Alexis T. Bell, and John M. Gregoire “Discovering Ce-rich Oxygen Evolution Catalysts, from High Throughput Screening to Water Electrolysis” Energy Environ. Sci., 2014,7, 682-688 .(DOI: 10.1039/c3ee43683g)
Screening results for an (Ni-Fe-Co-Ce)Ox system and identification of the new family of Ce-rich catalysts.
Catalyst performance resulting from inkjet-printed and electrodeposited catalysts using both high-throughput experimentation and conventional methods.
Oxygen evolution overpotentials at 10 mA/cm2 are nearly equivalent to those of the highest performing noble-metal based catalysts

## Slide 40: Materials Discovery
Rapid Technological Development of the Cerium-Rich Catalyst
Benchmarking
Integration into JCAP Prototypes
Performance Validation
Heterogeneous catalystis
HTE

## Slide 41: Materials Discovery
Rapid Technological Development of the Cerium-Rich Catalyst (continued)
Transmission Electron Microscope Imaging
The high-Ce catalyst is stable operating at pH 14 (XPS, SEM/EDS, EXAFS, XANES, Micro x-ray fluorescence)
The high-Ce catalyst is 2-phase
  transition metals (Ni, Fe, Co) mixed together in a single oxide (NiO) phase
  Ce is segregated to CeO2
  Both phases are well mixed nanometer crystallites
X-ray powder diffraction of powders calcined at 350 ⁰C and 450 ⁰ C confirm the bulk powder matches the TEM results
TEM analysis of similar catalyst compositions electrodeposited by Yun Cai display a finer crystallite size, but similar two-phase microstructure.

## Slide 42: Materials Discovery
Rapid Technological Development of the Cerium-Rich Catalyst (continued)
Extending the Catalyst Search
(Ni-Fe-Co-Ce)Ox
(Ni-Cu-Co-Ce)Ox
(Ni-Mn-Co-Ce)Ox
(Ni-Ta-Co-Ce)Ox
(Ni-Zn-Co-Ce)Ox
(Ni-Sn-Co-Ce)Ox
(Ni-La-Co-Ce)Ox
(Ni-Y-Co-Ce)Ox
Discovery of a new catalyst (Ni10La10Co30Ce50) with high catalytic activity and transparency
Catalyst is also stable for 100 h in a prototype test-bed electrolyzer (data not shown)

## Slide 43: Materials Discovery
Rapid Technological Development of the Cerium-Rich Catalyst (continued)
Tailoring High-Performing Catalysts for Light Absorbers
NiFeCoCeOx
NiLaCoCeOx
Deposition of catalyst materials directly onto light absorbers

## Slide 44: Materials Discovery
…And More…
Efficient light Architectures
Tunable Light Absorbers
Earth abundant H2 Catalysts
Stable, efficient Photocathodes
OER catalyst Mechanisms
Fundamental catalyst studies

## Slide 45: Summary
JCAP’s Future Direction
Opportunities and Challenges
• greater than 10% efficient micro-wire water-splitting devices
• photocathode assemblies for combined carbon dioxide separation and reduction
• plasmonic effects in electrocatalysis
• high-throughput structure determinations (with JCESR and CMI)
2014 JCAP All-Hands Meeting