## Slide 1
JCESR: Next Generation Energy Storage
George Crabtree
Director, JCESR
Argonne National Laboratory
University of Illinois at Chicago
Outline
JCESR Vision, Mission and Legacies
Science and Prototypes Status and Outlook
Multivalent
Lithium-Sulfur
Macromolecular Organic Flow
Basic Energy Sciences Advisory Committee
June 10, 2016
Bethesda, MD

## Slide 2
Today
Lithium-ion batteries enable
the personal electronics revolution
Forever changed the way we interact
with people and information
Tomorrow
$20K electric cars
Displace gasoline cars
Replace foreign oil with domestic electricity
Reduce energy use and carbon emissions
Grid-scale electricity storage
Widespread deployment of wind and solar
Enhance reliability, flexibility, resilience
Uncouple instantaneous generation
from instantaneous demand
~ 2% of US energy
Personal electronics
28% of US energy
Transportation
39% of US energy
Electricity grid

## Slide 3
Transportation
GRID
$100/kWh
400 Wh/kg 400 Wh/L
800 W/kg 800 W/L
1000 cycles
80% DoD C/5
15 yr calendar life
EUCAR
$100/kWh
95% round-trip efficiency at C/5 rate
7000 cycles C/5
20 yr calendar life
Safety equivalent to a natural gas turbine
JCESR: Beyond Lithium-ion Batteries for Cars and the Grid
Vision
Transform transportation and the electricity grid
with high performance, low cost energy storage
Mission
Deliver electrical energy storage with five times the energy density and one-fifth the cost of today’s commercial batteries within five years
Legacies
A library of the fundamental science of the materials and phenomena of energy storage at atomic and molecular levels
Two prototypes, one for transportation and one for the electricity grid, that, when scaled up to manufacturing, have the potential to meet JCESR’s transformative goals
A new paradigm for battery R&D that integrates discovery science, battery design, research prototyping and manufacturing collaboration in a single highly interactive organization

## Slide 4
JCESR Creates a New Paradigm for Battery R&D
Multivalent Intercalation
Chemical Transformation
Non-Aqueous Redox Flow
CROSSCUTTING SCIENCE
Systems Analysis and Translation
Cell Design and Prototyping
Commercial Deployment
Battery Design
Research Prototyping
Manufacturing Collaboration
MATERIALS
PROJECT
Sprints
Discovery Science
++
TECHNO-ECONOMIC MODELING
“Building battery systems on the computer”
ELECTROCHEMICAL DISCOVERY LAB
https://www.youtube.com/watch?v=wEzsKJwYjDQ
Focus exclusively on beyond lithium ion
A single highly interactive organization

## Slide 5
JCESR Team
20 Institutional Partners, 180-200 Researchers

## Slide 6
JCESR’s Beyond Lithium-ion Concepts
Multivalent Intercalation
Chemical Transformation
Replace monovalent Li+ with
di- or tri-valent ions: Mg++, Ca++, Al+++, . . .
Double or triple capacity
Replace solid electrodes with liquid solutions or suspensions:
lower cost, higher capacity, greater flexibility
Non-aqueous Redox Flow
Mg++
Lithium-ion “Rocking Chair”
Li+ cycles between anode and cathode, storing and releasing energy
Replace intercalation with high energy chemical reaction: Li-S, Li-O, Na-S, . . .
e
Li+
Li metal anode
Sulfur
cathode

## Slide 7: Four Prototype Targets
Proof-of-concept Prototypes
Transportation
Grid
Organic
Redox Flow
TE modeling
Genome
Synthesis
EDL
Materials
Components
Integration
Li-Sulfur Stationary
Li-O
Li-S Flow
Air-Breathing Aqueous Sulfur
Science-Driven Outcomes
Multivalent
Mg++, . . .
Science-Driven Outcomes
Final Prototype Targets Selected Jan 2016

## Slide 8
Multivalent Intercalation
One working example: Mg++ in Chevrel phase Mo6S8,
Aurbach et al (2000), Levi et al (2006)
Concept
Replace Li+ with Mg++, Ca++, Zn++
Advantage: double the energy per ion transfer
++
e
MV metal
anode
Intercalation cathode
Organic electrolyte
Mg++
Ca++
Zn++
Why is progress so slow?
Too many candidates, too few winners
Inadequate fundamental understanding for rational design
Challenges
Many cathodes operate at low voltage  low energy density
Divalent ions move slowly in cathode  slow charge, discharge
Electrolytes decompose at desirable cathode voltages
Anode surface degradation on plating and stripping

## Slide 9: Cathode Design Team

## Slide 10: New Multi-Valent Cathodes using Materials Project
Zn voltage low
Al, Y rare
Mg good, Ca superior

## Slide 11: The Mobility Challenge: A Pattern Emerges
M1/8FePO4 (olivine)
M1/8Mn2O4 (spinel)
tet
oct
tet
tet
oct
oct
Li, Ca, Mg borderline
Li, Zn
M1/8CoO2 (layered)
tet
oct
oct
Li, Zn
Design: best mobility is found for materials where the percolating ion is not too comfortable in its original site as compared to the sites along the percolation path
Materials Design Rules for Multivalent Ion Mobility in Intercalation Structures
Z. Rong, R. Malik, P. Canepa, G. Sai Gautam, M. Liu, A. Jain, K. Persson, and G. Ceder, Chemistry of Materials 2015 27 (17), 6016-6021

## Slide 12: Stable Full Cell Cycling: TiS2 spinel and BL-V2O5
A High Capacity Thiospinel Cathode for Mg Batteries, X. Sun, P. Bonnick, V. Duffort, Z. Rong M. Liu, K. Persson, G. Ceder, and L. F. Nazar, submitted
Excellent performance for Mg in a sulfide spinel and validating design rules
A High Power Rechargeable Non-aqueous Multivalent Zn/V2O5 Battery P. Senguttuvan, S.-D. Han, S. Kim, A. L. Lipson, S. Tepavcevic, T. T. Fister, I. D. Bloom, A. K. Burrell, C. S. Johnson submitted.
Excellent rate and cycle performance for Zn in a bi-layered V2O5 and validating design rules
(Aurbach 2000, Levi 2006)
First stable full-cell cycling of Mg in two dense crystal lattices beyond Mo6S8

## Slide 13: Electrolytes: Fundamental Understanding of Ion Pairing Enables Rational Design of Stability and Stripping / Plating
Separately solvated
anion and cation
Dilute solution
Weak electrostatic attraction
Monovalent Li+
Ion paired
anion and cation
Concentrated solution
Strong electrostatic attraction
Divalent Mg++, Ca ++, Zn++

## Slide 14: Ion-pairing Shifts the Electrochemical Stability Window . . .
Qu and Persson, submitted
Exp: 4 V
TFSI
Exp: 2 V
BH4
Free anion reduces
Ion-paired anion reduces
Ion-paired Mg2+ reduces
increasing F, S, O
decreasing organic
Hahn and Zavadil, in preparation
. . . reduces TFSI- anion, Mg absorbs the electron and triggers TFSI- decomposition
Ion-paired anions reduce more easily than well-solvated anions
The Coupling between Stability and Ion Pair Formation in Magnesium Electrolytes from First-Principles Quantum Mechanics and Classical Molecular Dynamics, N. N. Rajput, X. Qu, N.Sa, A. K. Burrell, and K. A. Persson, JACS 2015 137 (9), 3411-3420

## Slide 15
Ion-pairing induces decomposition of TFSI- anion
reduces anodic stability
partially reduces Mg++ to Mg+
alters stripping / plating behavior at anode
BH4- anion is stable under ion-pairing
 Rational design route to control anodic stability
Electrochemical Stability
6 stable + 6 marginally stable
Chemical Decomposition
5 stable
Hydrolysis
3 stable
DTPA
DMSA
MDPA
DFSA
4 promising anions; one under synthesis and testing at Sandia
Understanding Decomposition Pathway
Enables Rational Design
TFSI- derivatives maintaining high anodic stability while substituting the C-S bond
X. Qu, K. Matthews, …E. Maginn, K. Persson, in preparation
Compare with Zn electrolytes
Strong ion-pairing with excellent plating/stripping
Solvent, not anion, sets anodic stability limits of most Zn electrolytes (except Acetonitrile)
Rational design  achieve this for Mg
Rajput and Han et al., ACS Interfaces 2016
experiment
modeling*
Computational and experimental anodic limits of Zn electrolytes

## Slide 16
Public release of JCESR MV data and app
14,615 New structures
15,789 VASP runs
10,119 calculations
2+ Million CPU hours
Materials
Project
5255 New Compounds
1467 MV Cathodes
+
Battery App
to analyze properties
Public release of JCESR Molecule Data and Apps
> 21,000 organic molecules
Multi-faceted search by
  Drawn substructure
  Selected base molecule or functional groups
  Redox potentials
Redox flow battery dashboard
  Explore solubility and price targets
  Aqueous and non-aqueous
Redox Flow Battery Dashboard
Molecules Explorer
May 11, 2016

## Slide 17
Lithium-Sulfur Challenges
e
Li+
Li metal anode
Sulfur
cathode
  S8 (s) + 16 Li ↔ 8 Li2S (s)
  U = 2.2 V vs Li
S
Li2S
Li2Sx
Li2S8
Li2S6
Li2S4
Li2S
?
Sx
2-
Polysulfides: Li2Sx
• soluble in electrolyte
• migrate to anode
• react with Li  precipitate
• depletes Li and S
• limits cycle life
Li-electrolyte side reaction
Depletes Li and electrolyte
Limits cycles
Conventional fix: large excess of Li and electrolyte
Li dendrite growth
• cycling roughens Li surface
• dendrites form and grow
• break off to deplete Li
• grow across electrolyte to
short cathode
Li dendrite
Plating
JCESR
membrane in contact with Li anode surface
Maintain coherent interface as Li strips and plates through membrane
JCESR
• “lean” electrolyte
• sparing solvation
• solvates Li and anion, but
not polysulfides
JCESR
Protective membrane
• blocks electrolyte
• allows Li conduction
anode
cathode
electrolyte
Functionalized graphene oxide membrane

## Slide 18
JCESR Prototypes Constructed and Tested Push State-of-the-Art
JCESR today: 1 Ah Li/S cell (6 layers)
  270% excess Li
  1.7 mLElectrolyte/gSulfur lean electrolyte
  > 4.5 mAh/cm2 areal charge density in cathode
JCESR targets
  < 100% excess Li
  1 mLElectrolyte/gSulfur
  > 8 mAh/cm2
1 M LiTFSI, 0.2 M LiNO3
DOL:DME (v/v)
Chen et al., in prep (2016)
Research
Industry SOA
JCESR today
JCESR target
JCESR today
JCESR target
Eroglu et al., J. Electrochem. Soc., 162(6) A982 (2015)

## Slide 19
Lean Electrolyte / Sparing Solvation
Sparingly solvating
Unexplored Space
JCESR Opportunity
70%
10%
10%
10%
Note: Rough estimation based on literatures published from 2014-2016
Chart: 
 | 8.5 | 0.25 | 0.25 | 1
1-3%
1-3%
Solid State
Everyone else
DOL-DME
85%
other
10%
ACN2-LiTFSI:HFE electrolyte directs Li-S discharge reaction along different pathway from DOL-DME
Li2Sx
S
Li2S
Li2S/S22-
Discharge time
Fraction of Sulfur Species
Li2Sx
S
Li2S
Li2S/S22-
Operando X-ray Absorption
Li2S6 has small solubility ACN2-LiTFSI:HFE
1000x smaller than conventional DOL:DME-LiTFSI
Relatively low solubility for S8
15 person Sprint underway to determine mechanism of ACN2-LiTFSI:HFE solvation
Promising new route to JCESR targets

## Slide 20
Why GO Membranes?
laminar assembly
chemically functional
compliant, flexible
high shear modulus
Li+
L ≈ 50 mm
d ≈ 0.7 nm
Li metal
Graphene Oxide Protective Membranes
Strategies
Cross-link to block solvent
Impregnate with fast ion conductor for Li+ transport
Li-graded interface to insure coherent contact
melt infused Li in porous GO creates coherent interface
Coherent interface maintained after cycling
melt diffused Li in porous GO
200 nm thick functionalized GO
Prior to cycling Li
After cycling 0.5 mm at 1 mA/cm2
200 nm thick fGO
melt diffused Li
cycled Li layer
Next 18 months
Integrate functionalized GO membranes with sparingly solvating ACN2-LiTFSI:HFE electrolytes
  These two innovations, with PEO multifunctional cathodes already under way, are capable of meeting JCESR’s Li-S goals
                1 mLElectrolyte/gSufur lean electrolyte
                < 100% excess Li
                8 mAh/cm2 areal capacity

## Slide 21
• Ultralow $/Ah cost of sulfur
• High solubility in water  4X the energy density of
V-redox solutions
Air-Breathing Aqueous Sulfur Flow Battery
Full cell reaction
2Na2S + O2↑+ 2H2SO4 ⇄ 2S + 2Na2SO4 + 2H2O
Aqueous anolyte (Na2S8-Na2S)
Acidic catholyte (Na2SO4+ H2SO4))
$0.50/kg
Materials cost
Aqueous anolyte (Li2S8-Li2S)
Alkaline catholyte (Li2SO4, LiOH-H2O)
$0.05/kg
Materials cost
Can <$1/kWh chemical cost enable seasonal electrochemical energy storage?
Capture summer solar energy, use in winter
~ 4M cubic meters of sulfur from oil sands Fort McMurray, Alberta
8M sulfur (16M e-)
JCESR work on nonAq S laid groundwork
Catholyte Deep Cycling

## Slide 22: Air-Breathing Aqueous Sulfur Flow Directions
OER/ORR voltage hysteresis at cathode
    Catalyst selection
    Simultaneous gas and fluid flow
Prototyping
TE Modeling
Aqueous polysulfide solubility and speciation
    From 8M S today to >20M S
Stable, low-cost
membranes
    Ceramic membrane to separate pH
    Polymer membranes for alkaline/alkaline cells

## Slide 23: In 2014, JCESR Introduced the Concept of Macromolecular-based Redox Electrolytes . . .
Electrode Particle Size
RAC
105-109 redox units
Colloid
RAP
10 -1000 redox unit
Polymer
RAO
2 -10
redox units
Oligomer
RAM
1 redox unit
Molecule
Advantages
Inexpensive
Recyclable
Design for
• Solubility
• Stability
• Activity
• Size selectivity
. . . and the field gains momentum as others follow our lead . . .
Synthesis and characterization of TEMPO- and viologen-polymers for water-based redox-flow batteries, Polym. Chem., 6, 7801-7811 (2015)
Poly(TEMPO)/Zinc Hybrid-Flow Battery: A Novel, Green, High Voltage, and Safe Energy Storage System, Adv. Mater. 28, 2238–2243 (2016)
Poly(boron-dipyrromethene)—A Redox-Active Polymer Class for Polymer Redox-Flow Batteries, Chem. Mater., Article ASAP Publication Date (Web): May 6, 2016

## Slide 24
Solvent
And
Electrolyte
Dynamics
Electrode Structure
Montoto, E. C.; Nagarjuna, G.; Lewis, J.; Moore, J.S.; Rodriguez-Lopez, J.; et. al., Science (In Review)
Burgess, M.; Moore, J.S. Rodríguez-López, J. et. al. Analyst 2016, In Press.
Electronic Interactions
Burgess, M; Assary, R.; Moore, J.S. Rodríguez-López, J. et. al. In preparation.
Burgess, M.; Moore, J.S.; Rodríguez-López, J. et. al. J. Electrochem. Soc. 2016, 163, H3006-H3013.
Addressing a New Materials Challenge: Multiple Fronts
Gavvalapalli, N.; Hui, J.; Moore, J.S.;
Rodriguez-Lopez, J. et. al. J. Am. Chem. Soc. 2014, 136, 16309.
Montoto, E. C.; Brushett, F.; Moore, J.S.; Rodríguez-López, J. In preparation.
Flow Battery
Performance

## Slide 25
Celgard
Inexpensive
off the shelf
Polymer Intrinsic Microporous (PIM) membranes developed in JCESR for Li-S polysulfide selectivity
Tunable pore size ~ 1 nm
Li et al., Nano Letters, 15, 5724 (2015)
JCESR’s Macromolecular Organic Flow Cell Directions
Full cells of all four types routinely cycled
Target for next 18 months
Primary: RAO-PIM for cost target
Secondary: RAP-Celgard for
cost -performance comparison
based on TE modeling

## Slide 26
JCESR has opened new avenues for energy storage
Chemical Transformation
Non-aqueous Redox Flow
e
Li+
Li metal anode
Sulfur
cathode
Discovered breakthrough sulfur-based storage concept that promises low cost
Enabled a completely new class of redox flow molecules based on macromolecules
Multivalent Intercalation
Mg++
Rational Design of Cathodes and Electrolytes
New Mg Cathodes with Stable, Full-cell Cycling
Opened the “Electrolyte genome” website to the whole scientific community

## Slide 27
JCESR Intellectual Property
44 invention disclosures
26 patent applications
First license to Blue Current
Other licenses under negotiation
Two startup companies by JCESR members
Nitash Balsara, Alex Teran and Joe DeSimone (UNC)
Inorganic-polymer hybrids for Li anode batteries
Villaluenga et al, PNAS 113, 52, (2015)
Robin Johnston, Michel Fouré, Brett Helms and Peter Frischmann
Lightweight energy storage
for the electrification of flight
Li et al, Nano Lett. 15, 5724 (2015)
Best All-around Team
Bay Area I-Corps competition
Blue Current
Sepion
Engage the private sector
Train next generation entrepreneurs
Build JCESR relationships

## Slide 28
Further Reading
JCESR Website
Interactive, visual, engaging
www.jcesr.org
Why Energy Storage May Be the Most Important Technology in the World Right Now
Forbes Apr 1, 2016
Frontiers of Energy
Nature Energy Jan 11, 2016
Ten experts, including JCESR’s George Crabtree, share their vision of coming energy challenges
Perspective: The Energy Storage Revolution
Nature Oct 28, 2015
How next-generation storage can change the car and the grid
Lithium Batteries: To the Limits of Lithium
Nature Oct 28, 2015
Why We Need
A Revolution in Energy Storage
PBS Jan 5, 2016

## Slide 29
Supplementary Slides

## Slide 30
Community and Congressional Outreach
  At launch: 45 Affiliates
  Now: 97 Affiliates in 25 States
Annual Affiliates Days
Argonne Mar 2014
UC-Chicago Innovation Exchange May 2015
Chicago area – Fall 2016
Affiliates Newsletter Oct 2015
http://www.jcesr.org/partnerships/affiliates/
Regional Events Since July 2015
Mississippi State University Aug 2015
Pacific Northwest Seattle Sep 2015
Bay Area Battery Summit Nov 3 2015
UT Arlington Feb 2016
Congressional Battery Energy Storage Caucus Reps Takano(D-CA) and Collins (R-NY)
Senate Science, Energy and Natural Resources Committee
June 8, 2016
Energy Summit
Phoenix ECS Oct 2015
Keynote: Under Sec’y Lynn Orr
Overviews by JCESR, JCAP and EFRCs
ACS Symposium on QTR
San Diego Mar 13, 2016
With Rep Jerry McNerney (D-CA)
https://twitter.com/RepMcNerney/status/710873658282090496
Berkeley Energy Summit
Nov 3, 2015
Briefing CA delegation
Mar 15, 2016
National Lab Day on the Hill
Apr 20, 2016

## Slide 31
Top Ten Papers
764 citations
19 Highly Cited Papers
top 1% for field
1 Hot Paper
top 0.1% for field
ISI Web of Science
May 5, 2016
JCESR Publications
Q2
Q1
Q4
Q3
Q2
Q1
Q4
Q3
Q2
Q1
Q4
Q3
Q2
Q1
Y1
Y2
Y3
Y4
to date
Cumulative Publications
Peer reviewed journals exclusive of proceedings
Q2
Q1
Q4
Q3
Q2
Q1
Q4
Q3
Q2
Q1
Q4
Q3
Q2
Q1
Y1
Y2
Y3
Y4
to date
Quarterly Publications
Peer reviewed journals exclusive of proceedings
2013
2014
2015
2016
to date
Citations/Year
0-5
5-10
10-15
15-20
>20
Papers by Journal Impact Factor
Journal Impact Factor

## Slide 32
Fruchterman-Reingold force-directed graph: springs between nodes
  Attractive force: number of collaborative papers
  Artificial repulsive force to keep nodes from collapsing
  Nodes near the center are most collaborative
Institutional Collaboration within JCESR
Matt Shapiro
Political Science
Illinois Institute of Technology
38% of JCESR papers collaborate across JCESR institutions

## Slide 33
Matt Shapiro
Political Science
Illinois Institute of Technology
Institutional Collaboration with the Broader Community
Collaboration with 58 non-JCESR institutions
Engaging the community
Tapping valuable resources

## Slide 34
Personal Collaboration within JCESR
Nodes near the center are more collaborative
Matt Shapiro
Political Science
Illinois Institute of Technology

## Slide 35
Matt Shapiro
Political Science
Illinois Institute of Technology
Personal Collaboration with the Broader Community
> 300 Non-JCESR collaborators
Building relationships
Tapping intellectual resources