## Slide 1
Materials by Design and Condensed Matter Connections to High Energy Physics
Mike Norman
Director, Materials Science Division
PI, Center for Emergent Superconductivity
Argonne National Laboratory
December 8, 2014

## Slide 2
Outline
Low Temperature Superconducting Detectors (TES, etc.)
Superconducting RF Cavities, Magnets & Undulators
Wide Band Gap g-ray Detectors
Monopoles, Anapoles, Skyrmions, Majoranas & Higgs
AdS/CFT and Tensor Networks
with special thanks to Val Novosad (TES), Thomas Proslier & Mike Pellin (SRF),
Mercouri Kanatzidis (wide band gap), Wai Kwok & Ulrich Welp (SC wires & magnets)

## Slide 3
Low Temperature Detectors (Joel Ullom, NIST, Aug. 2012 BES Workshop)

## Slide 4: Bolometric detector - thermal detector EM Radiation Temperature Change Electrical signal
CMB INFRARED X-RAY
Spectral range is defined by the absorber
General Idea
COMPONENTS: Absorber, Thermometer, Thermal link
an opportunity for broad-band imaging
Heat sink to bath

## Slide 5
TES components optimization
Electronic properties
Thermal properties
Materials
Mo/Au
(Proximity)
Geometry
Membrane
perforation
Membrane
Thickness
Edge effects
control
Mo: Fe
(Implantation)
Ti
(metal)
Computer modeling
Absorber
Spider
-
web structure
Antennas
(polarization
-
sensitive)
Transmission line
Planar filters
Optically active devices
Array testing
-
Characterization & design optimization
It takes time & expertise to make a deployable device

## Slide 6
2001: ACBAR
16 detectors
2007: SPT
960 detectors
2012: SPTpol
1536 detectors
2016: SPT-3G
15,324 detectors
Evolution of CMB TES detectors
Requires new approach for higher focal plane density
50x improvement
10x improvement
Add polarization

## Slide 7
CUORE is funded by the US (DOE and NSF) and EU (INFN)
988 x 750 gram crystals of natural TeO2 with thermistors
Future R&D: Better background suppression and particle identification
“Thermal” + “light” detectors to distinguish between 0nbb events and a particles
SC detectors as a candidate technology: ultimate energy resolution, scalable, multiplexing with SQUIDs, thermal and/or optical sensitivity
Materials with Tc 10-15 mK are needed
Neutrinoless double beta decay with CUORE
(The Cryogenic Underground Observatory for Rare Events)
D. R. Artusa et al., http://arxiv.org/abs/1407.1094

## Slide 8
Scheme of R & D detector activities for CUORE-IHE
(Y. G. Kolomensky et al)

## Slide 9
Energy discrimination with TES for X-ray scattering
Joel Ullom, NIST,
Aug. 2012 BES Workshop
Elastic (RXS)
Inelastic (RIXS)
Will allow for a 100 fold improvement in signal to noise ratio

## Slide 10
transition to superinsulating state (TiN)
transition to superconducting state (TiN)
Improved resolution from superconductor-insulator transition?
Baturina et al, EPL (2012)

## Slide 11
Performance limitations: fundamental understanding of dissipation mechanisms
Atomic Layer Deposition: synthesizing new materials and application to RF cavities
RF electromagnetic field inside the cavity:
screening currents -> dissipation
-> performance
Superconducting Radio-Frequency (SRF) Cavities
SRF Cavity Needs:
Higher Gradients, Currents
Lower operational costs
  Operating Temperature
  Dissipation
Lower Capital Costs – Nb, fabrication, etc.

## Slide 12: Niobium surfaces are complex and poorly controlled at the nanometer scale
45 nm
RF depth
Inclusions,
Hydride precipitates
Surface oxide
Nb2O5 5-10 nm
Interface: sub oxides NbO, NbO2
often not crystalline
(niobium-oxygen “slush”)
Interstitials dissolved in niobium (mainly O, some C, N, H)
Grain boundaries
Residue from chemical processing
Clean niobium
e- flow only in the top 45 nm
Probe the surface superconductivity (by tunneling, etc.)

## Slide 13: A basis to build new cavity layered structures that might allow for transformationally higher field gradients
Al
Nb
Nb
AlN
NbTiN
Layered structures raise the critical magnetic field at which vortex losses form.
ALD allows fabrication with atomic scale precision without regard to the aspect ratio.
We need to develop ALD synthetic chemistries for superconducting material growth.
NbTiN
AlN
NbTiN
AlN
AlN
Gurvevich, Appl. Phys. Lett. (2006)

## Slide 15: Superconductors at Work
Power Cables, Electric Grid
Motors, Generators
& Wind turbines
Magnetic
Energy Storage
Transportation
MagLev
Long Island
Medical
MRI
Fusion Energy
Superconducting RF cavities

## Slide 16: Envisioned specifications for technical applications
TARGET ‘Sweet spot’ for rotating machines and high field magnets
10 MA/cm2 at T ~ 30K in several H = 2 – 30 Teslas
Typical operational parameters in various superconductor applications
V. Selvamanickam, HTS4 Fusion Workshop, May 26-27, 2011, Karlsruhe, Germany
Notes: Target specs for improving current state-of-the-art HTS YBCO commercial coated conductors

## Slide 17: Doubling Jc in a Few Seconds with Oxygen Irradiation
T = 5 K
ɑ = 0.57
ɑ = 0.77
2500 fold increase in defect creation: 1x1013 O2+/cm2
• No reduction in Tc
• Doubling of Jc after 37 sec with a 17 nA beam current
• Largest enhancement in high fields: rotating machinery, transformers, magnets
M. Leroux (ANL)
A. Kayani (WMU)
Viable reel-to-reel manufacturing process

## Slide 18
Undulators: sources of partially coherent, tunable X-rays
commonly used in linear accelerators and storage rings
Based on deflection of relativistic electrons in a periodic magnetic structure
B0
Magnetic deflection parameter K
After: D. T. Attwood, http://ast.coe.berkeley.edu/sxreuv/
Emitted wavelength
Range of tunability, brilliance of X-ray beam increase with K
Highest possible on-axis magnetic field B0
Undulators

## Slide 19
V. Selvamanickam (Univ. Houston)
Addition of 15% zirconium to MOCVD grown YBCO:
Dense array of self-assembled BaZrO3 nano-rods
effective pinning of
extended vortex
sections
Research samples reach the requirements for undulators
Plane-view
Cross-section
c
~ 17 nm spacing, ~ 5 nm diameter

## Slide 20
Possible operation of HTSC at temperatures above 4.2 K
Complex, expensive cryogenics for current NbTi-undulators
~ 10 K: higher cooling power, simpler and cheaper operation
Y. Ivanyushenkov (ANL)

## Slide 21: Metal chalcogenide - metal halide hybrid: high density wide band gap materials for g-ray detection
Eg
MxQy
Chalcogenides
MXn
Halides
MxQyXz
Chalco-halides
Optimum range
1.6 < Eg < 2.5 eV
CB
VB
Bandgap too low
Bandgap too high
For example:
BiBr3 (Eg ~ 2.2 eV) + Bi2S3 (Eg ~ 1.1 eV)  2BiSBr (Eg ~ 1.95 eV)
BiSBr has a high density of 6.7 g/cm3 and a band gap of 1.95 eV
Kanatzidis & Chung (ANL)

## Slide 22: Accomplishments – crystal growth and characterization
  Initiated synthesis and growth experiments in the SbSeX and Hg3Q2X2 (Q = S, Se, Te; X = Cl, Br, I) family of promising materials.
  Hg3Te2Br2 phase possess the highest density in the Hg3Q2X2 family of 7.78 g/cm3 and an optical band gap of 2.5 eV.
  Single crystal growth of SbSeI: - 8 mm x 10 mm in dimensions.
  Single crystal growth for Hg3Te2Br2 - up to 3 x 3 x 2 mm3 in dimensions.
Single crystals of Hg3Te2Br2 grown by vapor transport (grid is 1 mm)
Hg3Te2Br2
SbSeI
SbSeI
Photoconductivity response
Kanatzidis & Chung (ANL)

## Slide 23
Evolutionary search for
new superconductors
(FeB series)
Kolmorgorov et al, PRL (2010)
Predicted Superconductivity in oP10-FeB4 (15-20K)

## Slide 24
Synthesized and found to have a Tc of 3K
(only known “hit” from a materials genome approach)
Gou et al, PRL (2013)

## Slide 25
Similarity of SC Phase Diagrams
heavy fermions
pnictides
organics
cuprates

## Slide 26
Yellow – the “metal”, Red – the “ligand”, Blue, Green – the “spacer”
A possible search strategy for new superconductors

## Slide 27
But an increased Tc leads
to a reduced phase stiffness
Beasley, MRS Bulletin (2011)

## Slide 28
Monopoles, Anapoles, Skyrmions, Majoranas and Higgs
Welcome to the New World of Condensed Matter Physics

## Slide 29
Higgs modes in superconductors and charge density waves
Transfer of weight from SC to CDW Higgs modes
with decreasing T in NbSe2 (Raman scattering)
Measson et al, PRB (2014)
SC Higgs oscillations seen in THz
pump-probe studies of NbTiN
Matsunaga et al, PRL (2013)

## Slide 30
Yusupov et al., Nat. Phys. (2010)
CDW order parameter domain creation and annihilation in TbTe3
as revealed by pump-probe studies (Kibble-Zurek mechanism)
pump-probe delay (ps)

## Slide 31
Multipole expansion of magnetic free energy in a solid where
m is the magnetic dipole moment; a the magnetic monopole;
t the toroidal (anapole) moment; q the magnetic quadrupole
Dubrovik & Tugushev, Phys Rep (2000)
Di Matteo, J Phys D (2012)
Spaldin et al, PRB (2013)
+ monopole - monopole z anapole z2 quadrupole

## Slide 32
Toroidal moments have been observed in LiCoPO4
(used as a cathode in Li-ion batteries!)
by optical second harmonic generation
Van Aken et al., Nature (2007)

## Slide 33
Leonard: Are you really going to be on NPR?
Sheldon: Yes, they’re interviewing me by phone from my office regarding the recent so-called discovery of magnetic monopoles in spin-ices. It’s pledge week and they’re trying to goose the ratings with a little controversy.
Magnetic Monopoles in Spin Ice

## Slide 34
Magnetic Monopole Defects in Artificial Spin Ice
imaged with Lorentz TEM
Phatak et al, PRB (2011)

## Slide 35
Emergent E8 Symmetry in an Ising Spin Chain (CoNb2O6)
Zamolodchikov, IJMPA (1989)
Coldea et al, Science (2010)

## Slide 36
Skyrmions in Co doped FeSi (top) and Sc doped Ba ferrite (bottom)
imaged by Lorentz TEM
Yu et al, Nature (2010)
Yu et al, PNAS (2012)

## Slide 37
Kitaev, Phys Usp (2001)
Fu & Kane, PRL (2008)
Lutchyn et al, PRL (2010)
Oreg et al, PRL (2010)
A junction between a topological insulator (or a wire with
strong spin-orbit coupling) and a superconductor
might localize a Majorana mode at their junction

## Slide 38
Mourik et al, Science (2012)
Majorana Fermions in an InSb nanowire on NbTiN ?
zero mode
↓

## Slide 39
Topological Quantum Computing by Braiding Majorana Fermions
Kitaev, Phys Usp (2001)
Nayak et al, RMP (2008)
Alicea, RPP (2012)
Beenakker, ARCMP (2013)

## Slide 40
Hartnoll, Science (2008); Sachdev, ARCMP (2012)
Holographic Approach – AdS/CFT
Map a strong coupling QFT on the boundary of an AdS4 space-time to a weak coupling gravity dual in the interior with m and T determined by a “black brane” at the center
AdS2 → CFT1
← RG Flow (UV to IR)

## Slide 41
Applications to Condensed Matter Physics (?)
(well, there have always been those resistant to change!)

## Slide 42
Scalar fields near the “black brane” can condense (holographic
superconductivity) leading to a change from AdS2 x R2 → AdS4
This change in geometry causes the “light cone” for spinors to open
up (plot 2) giving rise to quasiparticles, with a Majorana coupling of
the spinors to the scalar opening up a Bogoliubov gap (plots 3 and 4)
Faulkner et al, JHEP (2010)
Energy vs momentum

## Slide 43
Can AdS/CFT help with condensed matter gauge theories?
(slave bosons for Kondo lattice, RVB for cuprates, etc.)
AdS/CFT large N limit is different from a typical condensed matter physics large N limit
Condensed matter gauge fields are typically constraint fields
In particular, they do not have a “kinetic” energy
(that is, one is at “infinite” coupling)
3. Can we find an AdS dual to such theories?
Nayak, Phys Rev Lett (2000)
Lee, Nagaosa, Wen, Rev Mod Phys (2006)

## Slide 44
iPEPS simulations of t-J model for doped cuprates
(lower variational free energy than fixed node QMC)
U – uniform antiferromagnet (AF) + d-wave superconductor (dSC)
W5 – modulated AF + dSC + charge density wave (CDW)
W5AP – modulated AF + antiphase dSC + CDW
Corboz et al, PRL (2014)

## Slide 45
Tensor Networks for Lattice Gauge Theories
Tagliacozzo et al, PRX (2014); Rico et al, PRL (2014);
Buyens et al, PRL (2014); Banuls et al, JHEP & PoS (2013)
H – Hilbert space
HP – physical Hilbert space
D – low energy sector
(area law for entanglement)