## Slide 1
Soren Prestemon
Director
US Magnet Development Program
Lawrence Berkeley National Laboratory
The U.S. Magnet Development Program

## Slide 2: Outline
Context for high field accelerator magnet R&D
  Motivation
  P5 and the Accelerator R&D Subpanel recommendations
The US Magnet Development Program
  How we are structured
Technical status of each area
  Progress and current status
  Corresponding roadmap within the MDP plan
Summary

## Slide 3: Advanced superconducting accelerator magnet technology is critical for a future collider
A large Hadron collider entails...
A high intensity proton source,
Fast-cycling magnets for the injection chain,
New magnets - probably high-field
A new tunnel
  Exception: HE-LHC could reach Ecm=33TeV with 20T dipoles…
Dominant cost drivers for an pp collider: Magnets and tunnel
Barletta
Cost/performance is the critical metric

## Slide 4: The US HEP Superconducting Magnet Programs are now integrated into the US Magnet Development Program
HEPAP Accelerator R&D Subpanel recommendations

## Slide 5: The management structure of the MDP is clearly defined and the program is fully functioning
MDP Management Group
S. Prestemon, LBNL
G. Velev, FNAL (Deputy)
L. Cooley, FNAL
S. Gourlay, LBNL
D. Larbalestier, FSU
A. Zlobin, FNAL
Technical Advisory Committee
Andrew Lankford, UC Irvine – Chair
Davide Tommasini, CERN
Akira Yamamoto, KEK
Joe Minervini, MIT
Giorgio Apollinari, FNAL (LARP/Hi-Lumi)
Mark Palmer, BNL

## Slide 6: Initial technical roles of participants matched with strengths and interests
FSU
  Conductor R&D
  Leverage Bi-2212 and REBCO R&D Program
  Shared infrastructure – overpressure furnace for sub-scale coils
FNAL
  Primary focus and responsibility for Cos-Theta
LBNL
  Primary responsibility for CCT
  Lead mechanical support structure effort between labs
  Primary responsibility for HTS component
Significant leverage with other programs, e.g.
- FES (on high temperature superconductors)
- SBIR program
- Early Career Research Program
- University programs (e.g. Ohio State, Tufts, U. of Houston, MIT, Florida State/NHMFL)
Close connection with LARP/HL-LHC AUP

## Slide 7: Technical areas have leads who are responsible for coordination and planning
Magnets | Lead
Cosine-theta 4-layer | Sasha Zlobin
Canted Cosine theta | Diego Arbelaez
Bi2212 dipoles | Tengming Shen
REBCO dipoles | Xiaorong Wang
Technology area | LBNL lead | FNAL lead
Modeling & Simulation | Diego Arbelaez | Vadim Kashikhin
Training and diagnostics | Maxim Martchevsky | Stoyan Stoynev
Instrumentation and quench protection | Emmanuele Ravaioli | Thomas Strauss
Material studies – superconductor and structural materials properties | Ian Pong | Steve Krave
Cond Proc and R&D | Lance Cooley
Nb3Sn
HTS
Conductor R&D
Technology development

## Slide 8: We have initiated a two-prong approach to high field dipoles to explore the limits of Nb3Sn
A reference design based on a 4-layer cosine-theta magnet utilizing high-performance Nb3Sn
A path to explore innovative designs
  Starting with the canted cosine-theta (CCT), a different paradigm that integrates mechanical structure internally

## Slide 9: Overview of the Nb3Sn Milestone Plan, Highlighting the Cos(θ) Reference Magnet Development and the Innovation Route with CCT

## Slide 10: The Cosine-theta 4-layer magnet is proceeding well at FNAL, with first coil prepared for VPI
Lead: Sasha Zlobin
Coil parts provided by CERN
Traces by LBNL
Outer coil winding
Novel coil layout addressing midplane stresses and field quality
Preparations for VPI

## Slide 11: The CCT program is proceeding to systematically address technical issues
Progress on the Canted Cosine Theta:
  Tested CCT2 (NbTi) and CCT3 (Nb3Sn)
  Testing of CCT4 in June 2017
Mandrel fabrication developed at LBNL, now done by industry
Coil winding: <1 day/layer
Reaction: simple, scalable tooling
Reaction of second layer; could be done together with other layers
Fabrication of Nb3Sn/NbTi joints
VPI using simple, scalable tooling
Assembly into an Al shell
Magnet testing with a breadth of diagnostics
Pace of effort scaled with funding
Cosine-theta at FNAL has higher priority
Lead: Diego Arbelaez

## Slide 12: Two candidate HTS conductors are pursued to explore and push the limits of HTS for high-field dipole applications
Bi-2212
  Rutherford cables and sub-scale magnets in racetrack and CCT configuration
REBCO
  Cable characterization and dipole magnet development
CORC®, from Advanced Conductor Technologies, Inc.

## Slide 13: Overview of the HTS Milestone Plan, Highlighting the Bi-2212 Magnet Development and the REBCO Magnet Development

## Slide 14: Significant progress on the Bi2212 HTS magnet front: Leveraging overpressure boost in magnet configurations
Lead: Tengming Shen
LBNL Bi2212 magnets:
Dramatic improvements in conductor properties in last couple of years
Racetrack & CCT coils fabricated and pushed to their electrical, mechanical, and quench limits

## Slide 15: REBCO program developing quickly: conductor and cable characterization, magnet design and prototyping underway
C0b wound with wire #2
1000 A @ 77 K and
12400 A @ 4.2K,
Peak Je = 1198 A/mm2
Courtesy
Danko Van Der Laan,
Advanced Conductor Technologies, Inc.
Tooling developed for winding of 40-turn prtototype
Lead: Xiaorong Wang

## Slide 16: Backbone of the Program: Magnet Science and Development of Underpinning Technologies
Areas of focus:
Training studies
Modeling
Diagnostics, quench detection, protection
Develop infrastructure, e.g. insert testing
New materials – insulation, impregnation and structural
Design comparison and cost analysis to guide program
Improvements/advances from this part of the program are then integrated into the Nb3Sn and HTS magnets

## Slide 17: Overview of the Technology Development Milestone Plan, which Feeds the Nb3Sn and HTS Magnet Program Elements

## Slide 18: Numerous technology advances are essential to address the high field magnet challenge
Periodic Model
Full Model
Full 3D simulations – utilizing the computing cluster Lawrencium at LBNL
Ten-stack measurements provide critical materials properties
FNAL PPD and “low temperature loader”
Leads: Ian Pong & Steve Krave
Lucas Brouwer

## Slide 19: Advanced diagnostics are providing new and critical insight into the mechanisms of training and magnet performance
“Axial-Field Magnetic Quench Antenna for the Superconducting Accelerator Magnets”, M. Marchevsky, A. R. Hafalia, D. Cheng, S. Prestemon, G. Sabbi, H. Bajas, G. Chlachidze, IEEE Trans. Appl. Supercond. 25, 9500605 (2015), DOI: 10.1109/TASC.2014.2374536
Acoustic emissions for localization
Acoustic emissions as detectors
Warm-bore quench antennas
Leads: Maxim Marchevsky & Stoyan Stoynev

## Slide 20: Superconducting Materials Procurement and R&D is Critical for Program Success
Push performance limits of Nb3Sn and HTS conductors
based on magnet needs
Understand –
  Uniformity and reliability
  Scalability and future cost
Quantity | Target
Diameter | 0.7 to 1.2 mm; (hold @ 1.3)
Unit length | 95% yield at 150 m
Jc(16 T, 4.2K) | 1300 A/mm2 (best effort) 1240 in cable
Jc std. dev. | < 100 A/mm2
RRR | >100; >50 at cable edge or in strand rolled to 15% reduction
Cu:NC | 0.9 to 1.1 (e.g. 150/169)
DSE | <60 μm
HT duration | <240 hours
Lead: Lance Cooley
Initial specifications for Nb3Sn conductor
Intend to procure Bi2212 wire soon utilizing existing Bi powder from SBIR programs

## Slide 21: The MDP is being managed and reviewed for program coherence and technical strength

## Slide 22: We have an active program focused on advancing high-field LTS and HTS accelerator magnet technology for future pp colliders
We have…
  an MDP Plan that lays out our goals and a roadmap for achieving them, fully aligned with the P5 report and the HEPAP Accelerator R&D Subpanel report
  established an excellent Technical Advisory Committee to provide guidance on our program
  identified individuals who will lead and coordinate efforts within the program
  organized our first yearly workshop to work through the program, identify technical issues, and provide input for budgets moving forward
Our focus now is delivering on our near term goals –
  making the Cosine-theta 4-layer magnet a success – potential new record field
  progressing through technical issues with the CCT to see if potential can be achieved
  making real dipoles from HTS and integrating them with LTS
  procuring sufficient conductors for the program, and identifying opportunities for conductor R&D

## Slide 23: Backup slides

## Slide 24: Cost-effective high-field superconducting magnets are essential for a future collider
R&D

## Slide 25: Exciting advances in HTS properties, but cost remains a major hurdle
P. Lee, ASC/FSU
V. Selvamanickam, U. Houston

## Slide 26: The Program is guided by Driving Questions… related to performance
What is the nature of accelerator magnet training? Can we reduce or eliminate it?
What are the drivers and required operation margin for Nb3Sn and HTS accelerator magnets?
What are the mechanical limits and possible stress management approaches for Nb3Sn and 20 T LTS/HTS magnets?
What are the limitations on means to safely protect Nb3Sn and HTS magnets?

## Slide 27: The Program is guided by Driving Questions…related to cost
Can we provide accelerator quality Nb3Sn magnets in the range of 16 T?
Is operation at 16 T economically justified? What is the optimal operational field for Nb3Sn dipoles?
What is the optimal operating temperature for Nb3Sn and HTS magnets?
Can we build practical and affordable accelerator magnets with HTS conductor(s)?
Are there innovative approaches to magnet design that address the key cost drivers for Nb3Sn and HTS magnets that will shift the cost optimum to higher fields?

## Slide 28: The Program is guided by Driving Questions… related to conductor development
What are the near and long-term goals for Nb3Sn and HTS conductor development? What performance parameters in Nb3Sn and HTS conductors are most critical for high field accelerator magnets?